Certificate of Thorough Examination & NDT of Lifting Equipment This Certificate complies with the requirements of the Lifting Equipment Operations and Lifting Equipment Regulations

Client Name:; Hilong Oil Services & Engineering; Rig Number:; HL99; Job Number:; ATS-05-24-3200.

Date of Examination:; 06/06/2024; Date of Report:; 06/06/2024; Certificate No:; ATS-05-24-3200-156.

Serial Number:; QTY; Description; SWL; Date of last Thorough examination. X01 X02; 02; Fabricated Pad Eyes Pad Eye Dimension Thickness: 20 MM Pin Hole: 30 MM Length: 60 MM Height: 71 MM Location: Crossover clamp SN: XC2; 100 KGS; N/A. Reference Standard:; LEEA DOC 048:2015. Is this the first examination after Installation or assembly at a new site or location?; Was the examination carried out: Within an interval of 6 months? With an interval of 12 months? In accordance with an examination scheme? After the occurrence of exceptional circumstances?. YES; NO; √; YES; √; NO. YES; NO; √. If the answer to the above question is YES has the equipment been installed correctly?; YES; NO; YES; √; NO. YES; NO; √. Identification of any part found to have a defect which is or could not become a danger to persons and a description of the defect: (If none Sate NONE) NONE. Is the above a defect which is of immediate danger to persons:; YES; NO. Is the above a defect which is not yet but could become a danger to persons (If YES state the date by when); N/A. Particulars of any repair, renewal or alteration required to remedy the defect identified above: NONE. IS THIS EQUIPMENT SAFE TO OPERATE?; YES; √; NO. NDT Equipment Details. Standard; ASTM E709; Viewing Condition:; Colored Media; Method; WET. Yoke; AC; Serial No:; 201504044; Due Date; 04-07-2024. Vernier Caliper; Digital; Serial No:; 8914; Due Date; 04-07-2024. White Contrast; FLUXO: WCP-4; Batch No:; L230523/1; Due Date; 23-05-2028. Black Ink; FLUXO: Black magnetic ink-3; Batch No:; L230125/3; Due Date; 25-1-2025. NDT Results. Visual and MPI carried out for the above description and found free of surface defects at the time of inspection. Identification of any part found to have a defect and a description of the defect: NONE. Particulars of any repair, renewal or alteration required to remedy the defect identified above: NONE. Name of Inspector:; Name of person authenticating this report:. Aram Dlawar; Hasan Omran. Signature& Stamp:. Latest date by which next thorough examination must be carried out:05-12-2024.