| Client: |  | Hilong Oil Services & Engineering |  | Certificate Number: |  | ATS-05-24-3200- MPI-146 |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Rig Number: |  | HL99 |  | Job No: |  | ATS-05-24-3200 |  |
| Location: |  | Southern Rumila – RU-258 |  | Page No: |  | 01 of 01 |  |
| Date of Inspection: |  | 06-06-2024 |  | Next Inspection Date: |  | 05-12-2024 |  |
| Type of Inspection |  | Visual inspection & MPI (Wet Visible Method) |  | Ref. Standards: |  | ASTM E709, ASTM E 1444 |  |
| PICTORIAL: |  |  |  |  |  | Item Description: utility winch counter weight |  |
|  |  |  |  |  |  | Unit Serial Number: HL003 |  |
|  |  |  |  |  |  | Details of inspection method(s): Visible magnetic particle inspection |  |
|  |  |  |  |  |  | Inspection Results: MPI WAS CARRIED OUT ON THE CRITICAL AND WELDING AREAS OF THE ABOVE-MENTIONED ITEMS AND FOUND NO CRACKS OR RELEVANT INDICATIONS AT THE TIME OF INSPECTION. |  |
|  |  |  |  |  |  | Remarks: ACCEPTED |  |
| Inspection Equipment Details |  |  |  | Personnel Details |  |  | Company Stamp |
| Equipment | Ac yoke |  |  | Inspector: | Aram Dlawar |  |  |
| Serial Number | 201504044 |  |  | Qualifications | ASNT LEVEL II |  |  |
| Calibration Date: | 05-01-2024 |  |  | Date: | 06-06-2024 |  |  |
| Calibration Due: | 04-07-2024 |  |  | Signature: |  |  |  |
| Consumables | MAGNETIC PARTICLES INSPECTION |  |  |  |  |  |  |
| Maker and Model | FLUXO |  | FLUXO | Supervisor: | Hasan Omran |  |  |
| Type: | WCP-4 |  | Black magnetic ink-3 |  |  |  |  |
| Batch Number | L230523/1 |  | L230125/3 | Date: | 08-06-2024 |  |  |
| Expiry Date: | 23-05-2028 |  | 25-1-2025 |  |  |  |  |